

# [Carbon nanomaterials: a new sustainable solution to reduce the emerging environme...](https://assignbuster.com/carbon-nanomaterials-a-new-sustainable-solution-to-reduce-the-emerging-environmental-pollution-of-turbomachinery-noise-and-vibration/)

[](https://assignbuster.com/)[Health & Medicine](https://assignbuster.com/essay-subjects/health-n-medicine/)

## Introduction

Noise pollution is deemed as one of the four major types of environmental pollution apart from air, water, and solid waste pollutions, and it poses a significant influence on not only human health but also environmental damage. Noise can affect the nervous system, endanger human health, destroy the ecosystem, and pollute the environment, leading to the deaths or even extinctions of living things ( [Stephen and Mark, 2003](#B62) ; [Francis et al., 2009](#B20) ; [Mehdi et al., 2011](#B46) ). Turbomachinery, such as car engines, large fans, compressors, and centrifugal pumps, has become a major source of noise pollution ( [Forouharmajd et al., 2012](#B19) ; [Gabbert et al., 2014](#B21) ; [Sun et al., 2020a](#B65) ). Because of the need for turbomachinery to run continuously ( [Jia et al., 2019](#B28) ; [Chen et al., 2020](#B10) ) the noise pollution caused by turbomachinery also continues to rise, dramatically increasing the sound pressure to a point that exceeds the pain threshold surmountable by humans and animals alike. Noise pollution can not only cause detriment to people's hearing, sleep quality, psychology, and environment but also accelerate mechanical breakdown and affect the precision as well as service life of the equipment. Because turbomachinery is being developed along the path of larger power, higher rotation speed, and higher pressure, the noise pollution problems also continue to exacerbate. As such, these noise pollution problems have become one of the many environmental pollution problems that need to be solved urgently. Traditionally, turbomachinery's noise and vibration reductions have been handled from the perspectives of vibration source and transmission path using passive control measures ( [Davies et al., 1982](#B14) ; [Elsukov et al., 1984](#B16) ; [Bies et al., 1996](#B7) ; [Choi et al., 2003](#B12) ; [Coleman and Remington, 2007](#B13) ). With the advancement of materials science nowadays, more and more new materials have been utilized ( [Sarkar et al., 2009](#B54) ; [Shukla et al., 2015](#B59) ; [Isaias et al., 2017](#B27) ; [Liu et al., 2019](#B42) ; [Sun et al., 2020b](#B66) ). Carbon nanocomposites, such as carbon nanofibers, carbon nanotubes, and graphenes, are characterized by low density, high strength, and high elastic modulus, which give carbon nanocomposites their damping properties, compatibilities, noise and vibration absorption properties, and wide wave-absorbing frequency bands ( [Baughman, 2002](#B6) ; [Young et al., 2012](#B74) ; [Nieto et al., 2016](#B48) ), making them the most promising vibration and noise reduction composites. Existing practical research on carbon nanocomposites in turbomachinery vibration and noise reduction is predominantly predicated upon the damping properties as well as sound and vibration absorptions. In this paper, progresses and application prospects of carbon nanocomposites in the field of turbomachinery vibration and noise reduction were discussed in two ways—damping property and sound absorption property of carbon nanocomposites.

## Vibration and Noise Reduction Based on the Damping Property

The approach of reducing vibration and noise based on the damping property is one of the most critical means by which vibration and noise can be reduced in machinery ( [Hang et al., 1993](#B24) ; [Lavernia et al., 1995](#B38) ). In this approach, the vibration energy of the mechanical system is converted into other forms of energy (such as thermal energy, and deformation energy) so that the system can be recovered to the pre-stimulated state as quickly as possible. Currently, popular damping materials include viscoelastic damping materials, damping composite materials, metal damping materials, and intelligent damping materials. Carbon nanocomposites, such as carbon nanofibers, carbon nanotubes, and graphenes, have become the most promising composites for vibration and noise reduction due to their low densities, high strengths, and high elastic moduli.

Carbon fibers have been more and more widely used in the fields of aerospace and petrochemical and medical treatment ( [Sheehan et al., 1994](#B55) ; [Park and Kim, 2010](#B50) ), owing to their unique stabilities, elastic moduli, strengths, stiffness, thermal conductivities, and lightweightness ( [Ruland, 1990](#B53) ; [Keiji et al., 2004](#B31) ; [Wu et al., 2010](#B70) ). Nevertheless, the high stiffness of carbon-fiber composite materials could lead to relatively low damping performance, in which case original cracks will be quickly propagated under the actions of periodic loads and external shocks, eventually resulting in vibration, fatigue, and failure ( [Khan et al., 2011](#B32) ; [Fan et al., 2016](#B17) ). Hence, effective measures should be taken to enhance the damping properties of carbon fiber materials. Based on the laminate board structure of carbon fiber acoustic metamaterial, [He et al. (2017)](#B25) not only effectively improved the damping property of carbon fiber materials but also achieved an effective vibration suppression effect by applying the laminate board of acoustic metamaterials to an automobile door design. [Li et al. (2017)](#B39) found that laying flax fibers on the outermost layer of the composite can effectively improve the damping property of the carbon fiber-reinforced composite after studying the influence of flax fiber stacking sequence and carbon nanotube additives on the damping and mechanical properties of carbon fiber-reinforced composites. [Lin et al. (1984)](#B41) provided an important guidance for the design of carbon fiber composite materials for vibration and noise reduction after investigating the intrinsic frequency and specific damping capacity of carbon fiber composite plates using various vibration models. According to Han's research ( [Han and Chung, 2012](#B23) ), mixing discontinuous particulate-shaped and fibrous fillers between carbon fiber sheets can effectively enhance the damping performance of carbon fiber materials.

Carbon nanotube was first discovered by [Lijima (1991)](#B40) in 1991. Every carbon atom in a carbon nanotube is connected to three adjacent carbon atoms, forming a hexagonal grid structure ( [Henning and Salama, 1998](#B26) ). In 1994, the carbon nanotube was used by [Ajayan et al. (1994)](#B1) as reinforcement material for polymer nanocomposites for the first time. According to Zhang's research ( [Zhang et al., 2011](#B76) ), the mechanical properties of the carbon nanotube is much better than that of carbon fiber. Carbon nanotubes can increase the damping properties of materials to a certain extent and hence facilitate vibration and noise reduction of mechanical systems ( [Cao et al., 2005](#B8) ; [Liu et al., 2008](#B43) ; [Zhang et al., 2009](#B75) ). [Kundalwal and Meguid (2015)](#B37) studied the effects of carbon nanotubes on the composite's active constrained-layer damping and discovered that the damping performance of multifunctional nanocomposite structures can be effectively improved with wavy carbon nanotubes. [Ma et al. (1998)](#B45) prepared carbon nanotube/nano-silicon carbide ceramic matrix composites via the hot pressing approach and found that their flexural strengths and fracture toughness were increased by 10% in comparison to nano-silicon carbide ceramics prepared under the same conditions. [Fereidoon and Ashoory (2010)](#B18) studied the damping properties of various carbon nanotube polymer composites and pointed out that mixing carbon nanotube fillers in the resin can improve the damping property. [Johnson et al. (2011)](#B29) reported that the damping ratio of fiber composites can be well increased after adding carbon nanotubes to fiber composites. [Zhou et al. (2004)](#B79) found that carbon nanotube fillers can increase the stick–slip friction on the surface of nanotubes, thus increasing the material damping. A study by [Suhr and Koratkar (2008)](#B64) indicated that the friction energy dissipation generated by the sliding of carbon nanotubes on the polycarbonate matrix can increase the damping ratio of materials. Furthermore, results obtained from the study of [Cao et al. (2005)](#B8) showed that the overlapped position of the carbon nanotube–carbon nanotube enhances the viscous effect in the matrix, presenting a significant damping enhancement effect.

[Mittal and Chaudhry (2015)](#B47) concluded that graphenes can raise the damping properties of nanocomposites by approximately 70% based on their study concerning the relationship between the mechanical damping behaviors of graphene-reinforced polymer nanocomposites and the surface morphologies of graphene nanosheets. Moreover, rigorous analyses have also suggested that the graphene filler interface can reinforce the damping property of nanocomposites ( [Stankovich et al., 2006](#B61) ; [Singh et al., 2011](#B60) ; [Young et al., 2012](#B74) ). According to Kim's research ( [Kim et al., 2017](#B35) ), adding graphenes to polyurethane foams can contribute to the reduction of the polyfoam's cell size and the increase in the polyfoam's bending path, thereby enhancing its acoustic damping performance. [Sudeshna et al. (2017)](#B63) found that the water content of graphene oxides plays a critical role in the damping performance of graphene oxide films; specifically, the lower the water content, the higher the viscoelasticity, and the greater the damping ratio. [Tang et al. (2014)](#B67) studied the mechanical and damping properties of graphene oxide/epoxy resin composites and found that the impact strengths and the damping properties of the composites are significantly improved with the increase in graphene oxide content.

## Vibration and Noise Reduction Based on the Property of Sound and Vibration Absorption

Apart from utilizing materials with damping properties, those with noise and vibration absorption properties are also one of the main research focuses in the study of noise and vibration reduction using composite materials. The sound and vibration absorption properties of composites are such that different velocity gradients are generated from the energy of energy waves when sound and vibration waves propagate in a variety of media (such as air, and sound-absorbing materials). Meanwhile, movement between adjacent mediator molecules can produce viscous and friction forces, causing the energy wave to be dissipated after being converted into thermal energy ( [Kishor and Pawar, 2019](#B36) ). Along with the advancement of materials science, more and more composite materials have also been applied in the field of noise and vibration absorption ( [Dunne et al., 2017](#B15) ; [Yang and Sheng, 2017](#B72) ; [Zhao et al., 2018](#B78) ; [Yang et al., 2019](#B73) ; [Xie et al., 2020](#B71) ). Carbon nanocomposites, such as carbon nanofibers, carbon nanotubes, and graphenes, have become the most promising vibration and noise absorption composites, owing to their favorable compatibilities, excellent sound and vibration absorption properties, and wide wave absorption frequency band.

Carbon nanofiber is a kind of high-performance and sound-absorbing multiporous fiber material ( [Rodrfguez-Mirasol et al., 1993](#B52) ) that consists of a large number of interpenetrable micropores. Chen and Jiang ( [Chen and Jiang, 2007](#B11) ) found that the sound absorption performance of the activated carbon fiber composite is superior to that of other composites. Based on this, [Shen and Jiang (2016)](#B58) , [Shen and Jiang (2014a](#B56) , [b](#B57) ) established a sound absorption theory model of activated carbon fiber materials by referring to the circular tube theory model and tested the sound absorption coefficient of the activated carbon fiber sensed in the frequency range of 250–6, 300 Hz using a dual-channel impedance tube acoustic analyzer. The result showed that the established sound absorption theory model of activated carbon fiber materials can provide theoretical and technical supports for designing and developing activated-carbon-fiber-based sound absorption materials.

Carbon nanotubes with a high length–width ratio can present good sound absorption performance at low concentrations ( [Khosla and Gray, 2009](#B33) ). [Ayub et al. (2018)](#B3) found that sound absorptions are associated with the molecular interactions between sound waves and nanomaterials, which take place under a very high frequency. What is more, they ( [Ayub et al., 2017](#B2) ) also found that a 3-millimeter-thick carbon nanolayer can provide up to 10% of sound absorption in the frequency range of 0. 125–4 kHz. According to the study carried out by [Bandarian et al. (2011)](#B5) , the porous wall carbon nanotube can reinforce the sound absorption capability of materials. It has also been found from some studies ( [Verdejo et al., 2009](#B68) ; [Willemsen and Rao, 2015](#B69) ) that adding a low concentration of carbon nanotubes can improve the sound absorption performance of polyurethane foam. Based on the study performed by [Gu et al. (2018)](#B22) , the addition of porous wall carbon nanotubes can effectively improve the underwater sound absorption performance of polyurethane coatings. On this basis, [Kabir et al. (2020)](#B30) also added surfactants and carboxyl-functionalized multiwalled carbon nanotubes to the polydimethylsiloxane nanocomposite membrane for underwater sound absorption to improve the sound absorption performance of the nanocomposites.

Since the interface interaction between graphenes and the matrix material could have a significant impact on the morphology, mechanical property, and electrical property of the composite, the addition of graphene will exert a certain modifying effect on metals, semiconductors, ceramics, polymers, and biomaterials. Because of such, the material constituted by the single-layer carbon atoms can be extensively used in polymer composites ( [Kim et al., 2010](#B34) ), thin film displays ( [Bae et al., 2010](#B4) ), and semiconductor devices ( [Liu et al., 2017](#B44) ). Moreover, because of graphene's high strength and modulus, the modifier, which is supposed to turn graphene into polymer materials, is also responsible for giving the prepared composite high rigidity and surface density, hence contributing positively to the acoustic property of the composite. [Zhang and Xu (2011)](#B77) predicted the strong sound absorption properties of surface acoustic waves in a wide frequency range below terahertz on the basis of studying the sound absorption of graphene under the effect of sound waves. [Qamoshi and Rasuli (2016)](#B51) enhanced the sound absorption capacity of polymers at a specific frequency upon the addition of graphene oxides to the carbon fiber polymers. [Nine et al. (2017)](#B49) enhanced the noise absorption capacity of a honeycomb grid structure by controlling the porosity and sinuosity of oxidized graphene sheets. [Carolina et al. (2019)](#B9) found through their study that reduced graphene oxide can improve the thermal stability and sound absorption coefficient of aerogels, creating a new research orientation for the preparation of emerging materials with excellent thermal insulation and sound absorption properties.

## Conclusion and Perspective

Since turbomachinery is the most widely used general-purpose machine in mechanical engineering, its vibratory noise problem has always been seen as a major issue and, hence, a research focus. In order to address this problem, researchers have studied vibration and noise reduction based on the damping performance and sound absorption properties of such carbon nanocomposites as carbon nanofibers, carbon nanotubes, and graphenes. Due to the late start of its development and application, carbon nanocomposites still have deficiencies in comparison to traditional metal materials in terms of achieving high-quality continuous production. Furthermore, many materials are still under development, while the growth mechanism of some carbon nanomaterials is still unclear, and the structure of carbon composites cannot be adjusted and controlled arbitrarily. Hence, it is imperative to further study carbon composites with vibration and noise reduction properties as well as wearproof corrosion characteristics. In this way, carbon nanocomposites with special functions can be developed by giving full play to their excellent properties. Meanwhile, apart from damping as well as sound and vibration properties, multifunctional carbon nanocomposites featuring high temperature resistance, corrosion resistance, and wear resistance should be also developed, due to their prospects in becoming a dominant research focus and development trend pertaining to turbomachinery. In the future, the application of carbon nanocomposites in surface coatings, low sound and vibration composites, compound material bearing in the field of turbomachinery vibration, and noise reduction will become the hotspot.

## Author Contributions

XJ and ZZ contributed to the conception of the study. XJ and SL wrote the article. HM, TY, DW, and JO searched the information. SL and BC edited the article. All authors contributed to the article and approved the submitted version.

## Funding

This work was supported by the National Natural Science Foundation of China and Liaoning Province (U1608258), National Natural Science Foundation of China (No. 51876110), and Zhejiang Provincial Natural Science Foundation of China (No. LQ19E060011).

## Conflict of Interest

HM, TY, and KR were employed by the company Hangzhou Dalu Industry Co., Ltd. DW was employed by the company Hangzhou Oxygen Plant Group Co., Ltd.

The remaining authors declare that the research was conducted in the absence of any commercial or financial relationships that could be construed as a potential conflict of interest.

## References

Ajayan, P. M., Stephan, O., Colliex, C., and Trauth, D. (1994). Aligned carbon nanotubes arrays formed by cutting a polymer resin-nanotubes composite. *J. Science.* 265, 1212–1214. doi: 10. 1126/science. 265. 5176. 1212

[PubMed Abstract](https://pubmed.ncbi.nlm.nih.gov/17787587) | [CrossRef Full Text](https://doi.org/10.1126/science.265.5176.1212) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=P.+M.+Ajayan&author=O.+Stephan&author=C.+Colliex&author=D.+Trauth+&publication_year=1994&title=Aligned+carbon+nanotubes+arrays+formed+by+cutting+a+polymer+resin-nanotubes+composite&journal=J.+Science.&volume=265&pages=1212-1214)

Ayub, M., Zander, A. C., Howard, C. Q., Cazzolato, B. S., Huang, D. M., Shanov, V. N., et al. (2017). Normal incidence acoustic absorption characteristics of a carbon nanotube forest. *Appl. Acoust* . 127, 223–239. doi: 10. 1016/j. apacoust. 2017. 06. 012

[CrossRef Full Text](https://doi.org/10.1016/j.apacoust.2017.06.012) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=M.+Ayub&author=A.+C.+Zander&author=C.+Q.+Howard&author=B.+S.+Cazzolato&author=D.+M.+Huang&author=V.+N.+Shanov+&publication_year=2017&title=Normal+incidence+acoustic+absorption+characteristics+of+a+carbon+nanotube+forest&journal=Appl.+Acoust&volume=127&pages=223-239)

Ayub, M., Zander, A. C., Huang, D. M., Howard, C. Q., and Cazzolato, B. S. (2018). Molecular dynamics simulations of acoustic absorption by a carbon nanotube. *Phys. Fluids* . 30: 066101. doi: 10. 1063/1. 5026528

[CrossRef Full Text](https://doi.org/10.1063/1.5026528) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=M.+Ayub&author=A.+C.+Zander&author=D.+M.+Huang&author=C.+Q.+Howard&author=B.+S.+Cazzolato+&publication_year=2018&title=Molecular+dynamics+simulations+of+acoustic+absorption+by+a+carbon+nanotube&journal=Phys.+Fluids&volume=30&pages=066101)

Bae, S., Kim, H., Lee, Y. B., Xu, X. f., Park, J. S., Zheng, Y., et al. (2010). Roll-to-roll production of 30-inch graphene films for transparent electrodes. *J. Nat. nanotechnol* . 5, 574–578. doi: 10. 1038/nnano. 2010. 132

[PubMed Abstract](https://pubmed.ncbi.nlm.nih.gov/20562870) | [CrossRef Full Text](https://doi.org/10.1038/nnano.2010.132) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=S.+Bae&author=H.+Kim&author=Y.+B.+Lee&author=X.+f.+Xu&author=J.+S.+Park&author=Y.+Zheng+&publication_year=2010&title=Roll-to-roll+production+of+30-inch+graphene+films+for+transparent+electrodes&journal=J.+Nat.+nanotechnol&volume=5&pages=574-578)

Bandarian, M., Shojaei, A., and Rashidi, A. M. (2011). Thermal, mechanical and acoustic damping properties of flexible open-cell polyurethane/multi-walled carbon nanotube foams: effect of surface functionality of nanotubes. *Polym. Int* . 60, 475–482. doi: 10. 1002/pi. 2971

[CrossRef Full Text](https://doi.org/10.1002/pi.2971) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=M.+Bandarian&author=A.+Shojaei&author=A.+M.+Rashidi+&publication_year=2011&title=Thermal,+mechanical+and+acoustic+damping+properties+of+flexible+open-cell+polyurethane%2Fmulti-walled+carbon+nanotube+foams%3A+effect+of+surface+functionality+of+nanotubes&journal=Polym.+Int&volume=60&pages=475-482)

Baughman, R. H. (2002). Carbon nanotubes-the route toward application. *Science* 297, 787–792. doi: 10. 1126/science. 1060928

[PubMed Abstract](https://pubmed.ncbi.nlm.nih.gov/12161643) | [CrossRef Full Text](https://doi.org/10.1126/science.1060928) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=R.+H.+Baughman+&publication_year=2002&title=Carbon+nanotubes-the+route+toward+application&journal=Science&volume=297&pages=787-792)

Bies, D. H., Hansen, C. H., and Campbell, R. H. (1996). Engineering noise control. *J. Acous. Soc. Am* . 100: 1279. doi: 10. 1121/1. 416038

[CrossRef Full Text](https://doi.org/10.1121/1.416038) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=D.+H.+Bies&author=C.+H.+Hansen&author=R.+H.+Campbell+&publication_year=1996&title=Engineering+noise+control&journal=J.+Acous.+Soc.+Am&volume=100&pages=1279)

Cao, A., Dickrell, P., Sawyer, W., Ghasemi-Nejhad, M., Ajayan, P. (2005). Super-compressible foamlike carbon nanotubes films. *J. Science.* 310, 1307–1310. doi: 10. 1126/science. 1118957

[PubMed Abstract](https://pubmed.ncbi.nlm.nih.gov/16311330) | [CrossRef Full Text](https://doi.org/10.1126/science.1118957) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=A.+Cao&author=P.+Dickrell&author=W.+Sawyer&author=M.+Ghasemi-Nejhad&author=P.+Ajayan+&publication_year=2005&title=Super-compressible+foamlike+carbon+nanotubes+films&journal=J.+Science.&volume=310&pages=1307-1310)

Carolina, S. H., Peco, N., Romero, A., José L, V., Luz, S. S. (2019). PVA/nanoclay/graphene oxide aerogels with enhanced sound absorption properties. *J. Appl. Acoust.* 156, 40–45. doi: 10. 1016/j. apacoust. 2019. 06. 023

[CrossRef Full Text](https://doi.org/10.1016/j.apacoust.2019.06.023) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=S.+H.+Carolina&author=N.+Peco&author=A.+Romero&author=V.+José+L&author=S.+S.+Luz+&publication_year=2019&title=PVA%2Fnanoclay%2Fgraphene+oxide+aerogels+with+enhanced+sound+absorption+properties&journal=J.+Appl.+Acoust.&volume=156&pages=40-45)

Chen, D. S., Lin, Z., and Liu, Q. (2020). Numerical investigation of the valve-induced disturbance of the performance of a swirl meter. *Measurement* . 162: 107957. doi: 10. 1016/j. measurement. 2020. 107957

[CrossRef Full Text](https://doi.org/10.1016/j.measurement.2020.107957) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=D.+S.+Chen&author=Z.+Lin&author=Q.+Liu+&publication_year=2020&title=Numerical+investigation+of+the+valve-induced+disturbance+of+the+performance+of+a+swirl+meter&journal=Measurement&volume=162&pages=107957)

Chen, Y., and Jiang, N. (2007). Carbonized and activated non-wovens as high-performance acoustic materials. *Textile Res. J* . 77, 785–791. doi: 10. 1177/0040517507080691

[CrossRef Full Text](https://doi.org/10.1177/0040517507080691) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=Y.+Chen&author=N.+Jiang+&publication_year=2007&title=Carbonized+and+activated+non-wovens+as+high-performance+acoustic+materials&journal=Textile+Res.+J&volume=77&pages=785-791)

Choi, J. S., Mclaughlin, D. K., and Thompson, D. E. (2003). Experiments on the unsteady flow field and noise generation in a centrifugal pump impeller. *J. Sound Vibration* 263, 493–514. doi: 10. 1016/S0022-460X(02)01061-1

[CrossRef Full Text](https://doi.org/10.1016/S0022-460X(02)01061-1) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=J.+S.+Choi&author=D.+K.+Mclaughlin&author=D.+E.+Thompson+&publication_year=2003&title=Experiments+on+the+unsteady+flow+field+and+noise+generation+in+a+centrifugal+pump+impeller&journal=J.+Sound+Vibration&volume=263&pages=493-514)

Coleman, R., and Remington, P. J. (2007). “ Active control of noise and vibration,” in *Noise and Vibration Control Engineering* , eds L. István Vér and L. L. Beranek (Hoboken, NJ: John, Wiley and Sons, Inc), 18.

[Google Scholar](http://scholar.google.com/scholar_lookup?author=R.+Coleman&author=P.+J.+Remington+&publication_year=2007&title=“ Active+control+of+noise+and+vibration,”&journal=Noise+and+Vibration+Control+Engineering&pages=18)

Davies, P. O., Heckl, M., and Koopman, G. L. (1982). “ Noise generation and control in mechanical engineering,” in *CISM* , ed G. Bianchi (Vienna: Springer Press), 276.

[Google Scholar](http://scholar.google.com/scholar_lookup?author=P.+O.+Davies&author=M.+Heckl&author=G.+L.+Koopman+&publication_year=1982&title=“ Noise+generation+and+control+in+mechanical+engineering,”&journal=CISM&pages=276)

Dunne, R., Desai, D., and Sadiku, R. (2017). A review of the factors that influence sound absorption and the available empirical models for fibrous materials. *Acoust. Aust* . 45, 453–469. doi: 10. 1007/s40857-017-0097-4

[CrossRef Full Text](https://doi.org/10.1007/s40857-017-0097-4) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=R.+Dunne&author=D.+Desai&author=R.+Sadiku+&publication_year=2017&title=A+review+of+the+factors+that+influence+sound+absorption+and+the+available+empirical+models+for+fibrous+materials&journal=Acoust.+Aust&volume=45&pages=453-469)

Elsukov, V. A., Golovnin, P. A., and Kramarovskii, S. V. (1984). Universal active compensation apparatus for suppressing noise and vibration. *Measurement Techniques* 27, 461–462. doi: 10. 1007/BF00838699

[CrossRef Full Text](https://doi.org/10.1007/BF00838699)

Fan, W., Li, J. L., Chen, L., Wang, H., Guo, D. D., and Liu, J. X. (2016). Influence of thermo-oxidative aging on vibration damping characteristics of conventional and graphene-based carbon fiber fabric composites. *Polymer Compos* . 37, 2871–2883. doi: 10. 1002/pc. 23484

[CrossRef Full Text](https://doi.org/10.1002/pc.23484) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=W.+Fan&author=J.+L.+Li&author=L.+Chen&author=H.+Wang&author=D.+D.+Guo&author=J.+X.+Liu+&publication_year=2016&title=Influence+of+thermo-oxidative+aging+on+vibration+damping+characteristics+of+conventional+and+graphene-based+carbon+fiber+fabric+composites&journal=Polymer+Compos&volume=37&pages=2871-2883)

Fereidoon, A., and Ashoory, M. (2010). Damping augmentation of epoxy using carbon nanotubes. *Int. J. Polym. Mater.* 60, 11–26. doi: 10. 1080/00914037. 2010. 504152

[CrossRef Full Text](https://doi.org/10.1080/00914037.2010.504152) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=A.+Fereidoon&author=M.+Ashoory+&publication_year=2010&title=Damping+augmentation+of+epoxy+using+carbon+nanotubes&journal=Int.+J.+Polym.+Mater.&volume=60&pages=11-26)

Forouharmajd, F., Nassiri, P., and Monazzam, M. R. (2012). Noise pollution of air compressor and its noise reduction procedures by using an enclosure. *Int. J. Env. Health Eng.* 1: 20. doi: 10. 4103/2277-9183. 96143

[CrossRef Full Text](https://doi.org/10.4103/2277-9183.96143) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=F.+Forouharmajd&author=P.+Nassiri&author=M.+R.+Monazzam+&publication_year=2012&title=Noise+pollution+of+air+compressor+and+its+noise+reduction+procedures+by+using+an+enclosure&journal=Int.+J.+Env.+Health+Eng.&volume=1&pages=20)

Francis, C. D., Ortega, C. P., and Cruz, A. (2009). Noise pollution changes avian communities and species interactions. *Curr. Biol* . 19: 52. doi: 10. 1016/j. cub. 2009. 06. 052

[PubMed Abstract](https://pubmed.ncbi.nlm.nih.gov/19631542) | [CrossRef Full Text](https://doi.org/10.1016/j.cub.2009.06.052) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=C.+D.+Francis&author=C.+P.+Ortega&author=A.+Cruz+&publication_year=2009&title=Noise+pollution+changes+avian+communities+and+species+interactions&journal=Curr.+Biol&volume=19&pages=52)

Gabbert, U., Duvigneau, F., and Shan, J. J. (2014). “ Active and passive measures to reduce the noise pollution of combustion engines,” *11th IEEE International Conference on Information and AutomationAt: Hailar* (Hulun Buir, Inner Mongolia), 1072–1077. doi: 10. 1109/ICInfA. 2014. 6932808

[CrossRef Full Text](https://doi.org/10.1109/ICInfA.2014.6932808) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=U.+Gabbert&author=F.+Duvigneau&author=J.+J.+Shan+&publication_year=2014&title=“ Active+and+passive+measures+to+reduce+the+noise+pollution+of+combustion+engines,”&journal=11th+IEEE+International+Conference+on+Information+and+AutomationAt%3A+Hailar&pages=1072-1077)

Gu, B. E., Huang, C. Y., Shen, T. H., and Lee, Y. L. (2018). Effects of multiwall carbon nanotube addition on the corrosion resistance and underwater acoustic absorption properties of polyurethane coatings. *Prog. Org. Coat* . 121, 226–235. doi: 10. 1016/j. porgcoat. 2018. 04. 033

[CrossRef Full Text](https://doi.org/10.1016/j.porgcoat.2018.04.033) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=B.+E.+Gu&author=C.+Y.+Huang&author=T.+H.+Shen&author=Y.+L.+Lee+&publication_year=2018&title=Effects+of+multiwall+carbon+nanotube+addition+on+the+corrosion+resistance+and+underwater+acoustic+absorption+properties+of+polyurethane+coatings&journal=Prog.+Org.+Coat&volume=121&pages=226-235)

Han, S., and Chung, D. D. L. (2012). Mechanical energy dissipation using carbon fiber polymer-matrix structural composites with filler incorporation. *Mater. Sci* . 47, 2434–2453. doi: 10. 1007/s10853-011-6066-7

[CrossRef Full Text](https://doi.org/10.1007/s10853-011-6066-7) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=S.+Han&author=D.+D.+L.+Chung+&publication_year=2012&title=Mechanical+energy+dissipation+using+carbon+fiber+polymer-matrix+structural+composites+with+filler+incorporation&journal=Mater.+Sci&volume=47&pages=2434-2453)

Hang, J., Perez, R. J., and Lavernia, E. J. (1993). Documentation of damping capacity of metallic, ceramic and metal-matrix composite materials. *J. Mater. Sci* . 28, 2395–2404. doi: 10. 1007/BF01151671

[CrossRef Full Text](https://doi.org/10.1007/BF01151671) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=J.+Hang&author=R.+J.+Perez&author=E.+J.+Lavernia+&publication_year=1993&title=Documentation+of+damping+capacity+of+metallic,+ceramic+and+metal-matrix+composite+materials&journal=J.+Mater.+Sci&volume=28&pages=2395-2404)

He, Z. C., Xiao, X., and Eric, L. I. (2017). Design for structural vibration suppression in laminate acoustic metamaterials. *Comp. Part B Eng* . 131, 237–252. doi: 10. 1016/j. compositesb. 2017. 07. 076

[CrossRef Full Text](https://doi.org/10.1016/j.compositesb.2017.07.076) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=Z.+C.+He&author=X.+Xiao&author=L.+I.+Eric+&publication_year=2017&title=Design+for+structural+vibration+suppression+in+laminate+acoustic+metamaterials&journal=Comp.+Part+B+Eng&volume=131&pages=237-252)

Henning, T. H., and Salama, F. (1998). Carbon in the universe. *Science* 282: 2204. doi: 10. 1126/science. 282. 5397. 2204

[PubMed Abstract](https://pubmed.ncbi.nlm.nih.gov/9856936) | [CrossRef Full Text](https://doi.org/10.1126/science.282.5397.2204) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=T.+H.+Henning&author=F.+Salama+&publication_year=1998&title=Carbon+in+the+universe&journal=Science&volume=282&pages=2204)

Isaias, H. C., Christopher, J. W., and Liu, H. (2017). Advanced materials for the impeller in an ORC radial microturbine. *Energy Procedia* . 129, 1047–1054. doi: 10. 1016/j. egypro. 2017. 09. 241

[CrossRef Full Text](https://doi.org/10.1016/j.egypro.2017.09.241) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=H.+C.+Isaias&author=J.+W.+Christopher&author=H.+Liu+&publication_year=2017&title=Advanced+materials+for+the+impeller+in+an+ORC+radial+microturbine&journal=Energy+Procedia&volume=129&pages=1047-1054)

Jia, X. Q., Zhu, Z. C., Yu, X. L., and Zhang, Y. L. (2019). Internal unsteady flow characteristics of centrifugal pump based on entropy generation rate and vibration energy. *Proc. Inst. Mech. Eng. Part E J. Process Mech. Eng* . 233, 456–473. doi: 10. 1177/0954408918765289

[CrossRef Full Text](https://doi.org/10.1177/0954408918765289) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=X.+Q.+Jia&author=Z.+C.+Zhu&author=X.+L.+Yu&author=Y.+L.+Zhang+&publication_year=2019&title=Internal+unsteady+flow+characteristics+of+centrifugal+pump+based+on+entropy+generation+rate+and+vibration+energy&journal=Proc.+Inst.+Mech.+Eng.+Part+E+J.+Process+Mech.+Eng&volume=233&pages=456-473)

Johnson, R. J., Tang, J., and Pitchumani, R. (2011). Characterization of damping in carbon-nanotube filled fiberglass reinforced thermosetting-matrix composites. *Mater. Sci* . 46, 4545–4554. doi: 10. 1007/s10853-011-5349-3

[CrossRef Full Text](https://doi.org/10.1007/s10853-011-5349-3) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=R.+J.+Johnson&author=J.+Tang&author=R.+Pitchumani+&publication_year=2011&title=Characterization+of+damping+in+carbon-nanotube+filled+fiberglass+reinforced+thermosetting-matrix+composites&journal=Mater.+Sci&volume=46&pages=4545-4554)

Kabir, I. I., Fu, Y., Souza, N. D., Baena, J. C., Yang, W., Yeoh, G. H., et al. (2020). PDMS/MWCNT nanocomposite films for underwater sound absorption applications. *J. Mater. Sci* 55, 5048–5063. doi: 10. 1007/s10853-020-04349-4

[CrossRef Full Text](https://doi.org/10.1007/s10853-020-04349-4) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=I.+I.+Kabir&author=Y.+Fu&author=N.+D.+Souza&author=J.+C.+Baena&author=W.+Yang&author=G.+H.+Yeoh+&publication_year=2020&title=PDMS%2FMWCNT+nanocomposite+films+for+underwater+sound+absorption+applications&journal=J.+Mater.+Sci&volume=55&pages=5048-5063)

Keiji, O., Tomoyuki, S., and Makoto, M. (2004). Strength in concrete reinforced with recycled CFRP pieces. *Composites* 36, 893–902. doi: 10. 1016/j. compositesa. 2004. 12. 009

[CrossRef Full Text](https://doi.org/10.1016/j.compositesa.2004.12.009) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=O.+Keiji&author=S.+Tomoyuki&author=M.+Makoto+&publication_year=2004&title=Strength+in+concrete+reinforced+with+recycled+CFRP+pieces&journal=Composites&volume=36&pages=893-902)

Khan, S. U., Li, C. Y., Siddiqui, N. A., and Kim, J. K. (2011). Vibration damping characteristics of carbon fiber-reinforced composites containing multi-walled carbon nano-tubes. *Compos. Sci. Technol* . 71, 1486–1494. doi: 10. 1016/j. compscitech. 2011. 03. 022

[CrossRef Full Text](https://doi.org/10.1016/j.compscitech.2011.03.022) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=S.+U.+Khan&author=C.+Y.+Li&author=N.+A.+Siddiqui&author=J.+K.+Kim+&publication_year=2011&title=Vibration+damping+characteristics+of+carbon+fiber-reinforced+composites+containing+multi-walled+carbon+nano-tubes&journal=Compos.+Sci.+Technol&volume=71&pages=1486-1494)

Khosla, A., and Gray, B. L. (2009). Preparation, characterization and micromolding of multi-walled carbon nanotube polydimethylsiloxane conducting nanocomposite polymer. *Mater. Lett* . 63, 1203–1206. doi: 10. 1016/j. matlet. 2009. 02. 043

[CrossRef Full Text](https://doi.org/10.1016/j.matlet.2009.02.043) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=A.+Khosla&author=B.+L.+Gray+&publication_year=2009&title=Preparation,+characterization+and+micromolding+of+multi-walled+carbon+nanotube+polydimethylsiloxane+conducting+nanocomposite+polymer&journal=Mater.+Lett&volume=63&pages=1203-1206)

Kim, H., Abdala, A. A., and Macosko, C. W. (2010). Graphene/polymer nanocomposites. *Macromolecules* 43, 6515–6530. doi: 10. 1021/ma100572e

[CrossRef Full Text](https://doi.org/10.1021/ma100572e) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=H.+Kim&author=A.+A.+Abdala&author=C.+W.+Macosko+&publication_year=2010&title=Graphene%2Fpolymer+nanocomposites&journal=Macromolecules&volume=43&pages=6515-6530)

Kim, J. M., Kim, D. H., Kim, J., Lee, J. W., and Kim, W. N. (2017). Effect of graphene on the sound damping properties of flexible polyurethane foams. *J. Macromol. Res* . 25, 1–7. doi: 10. 1007/s13233-017-5017-9

[CrossRef Full Text](https://doi.org/10.1007/s13233-017-5017-9) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=J.+M.+Kim&author=D.+H.+Kim&author=J.+Kim&author=J.+W.+Lee&author=W.+N.+Kim+&publication_year=2017&title=Effect+of+graphene+on+the+sound+damping+properties+of+flexible+polyurethane+foams&journal=J.+Macromol.+Res&volume=25&pages=1-7)

Kishor, K., and Pawar, S. J. (2019). A review on the taxonomy, factors associated with sound absorption and theoretical modeling of porous sound absorbing materials. *J. Porous Mater* . 26, 1795–1819. doi: 10. 1007/s10934-019-00774-2

[CrossRef Full Text](https://doi.org/10.1007/s10934-019-00774-2) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=K.+Kishor&author=S.+J.+Pawar+&publication_year=2019&title=A+review+on+the+taxonomy,+factors+associated+with+sound+absorption+and+theoretical+modeling+of+porous+sound+absorbing+materials&journal=J.+Porous+Mater&volume=26&pages=1795-1819)

Kundalwal, S. I., and Meguid, S. A. (2015). Effect of carbon nanotube waviness on active damping of laminated hybrid composite shells. *Acta Mech* . 226, 2035–2052. doi: 10. 1007/s00707-014-1297-8

[CrossRef Full Text](https://doi.org/10.1007/s00707-014-1297-8) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=S.+I.+Kundalwal&author=S.+A.+Meguid+&publication_year=2015&title=Effect+of+carbon+nanotube+waviness+on+active+damping+of+laminated+hybrid+composite+shells&journal=Acta+Mech&volume=226&pages=2035-2052)

Lavernia, E. J., Perez, R. J., and Zhang, J. (1995). *Metall. Mater. Trans* . 26, 2803–2818. doi: 10. 1007/BF02669639

[CrossRef Full Text](https://doi.org/10.1007/BF02669639)

Li, Y., Cai, S., and Huang, X. (2017). Multi-scaled enhancement of damping property for carbon fiber reinforced composites. *Compos. Sci. Technol* . 143, 89–97. doi: 10. 1016/j. compscitech. 2017. 03. 008

[CrossRef Full Text](https://doi.org/10.1016/j.compscitech.2017.03.008) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=Y.+Li&author=S.+Cai&author=X.+Huang+&publication_year=2017&title=Multi-scaled+enhancement+of+damping+property+for+carbon+fiber+reinforced+composites&journal=Compos.+Sci.+Technol&volume=143&pages=89-97)

Lijima, S. (1991). Helical microtubules of graphitic carbon. *Nature* 354: 56. doi: 10. 1038/354056a0

[CrossRef Full Text](https://doi.org/10.1038/354056a0) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=S.+Lijima+&publication_year=1991&title=Helical+microtubules+of+graphitic+carbon&journal=Nature&volume=354&pages=56)

Lin, D. X., Ni, R. G., and Adams, R. D. (1984). Predication and measurement of the vibrational damping parameters of carbon and glass fiber-reinforced plastics plates. *J. Compos. Mater.* 18, 132–152. doi: 10. 1177/002199838401800204

[CrossRef Full Text](https://doi.org/10.1177/002199838401800204) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=D.+X.+Lin&author=R.+G.+Ni&author=R.+D.+Adams+&publication_year=1984&title=Predication+and+measurement+of+the+vibrational+damping+parameters+of+carbon+and+glass+fiber-reinforced+plastics+plates&journal=J.+Compos.+Mater.&volume=18&pages=132-152)

Liu, H. Y., Zhang, X. X., Peng, T., Li, X. H., and Yan, Q. Z. (2019). Preparation of large-scale Ti3SiC2 ceramic impeller with complex shape basing on the optimization of sintering manner. *Ceramics Intern* . 45, 22308–22315. doi: 10. 1016/j. ceramint. 2019. 07. 258

[CrossRef Full Text](https://doi.org/10.1016/j.ceramint.2019.07.258) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=H.+Y.+Liu&author=X.+X.+Zhang&author=T.+Peng&author=X.+H.+Li&author=Q.+Z.+Yan+&publication_year=2019&title=Preparation+of+large-scale+Ti3SiC2+ceramic+impeller+with+complex+shape+basing+on+the+optimization+of+sintering+manner&journal=Ceramics+Intern&volume=45&pages=22308-22315)

Liu, Y., Qian, W., Zhang, Q., Cao, A., Li, Z., Zhou, W., et al. (2008). Hierarchical agglomerates of carbon nanotubes as high-pressure cushions. *J. Nano Lett.* 8, 1323–1327. doi: 10. 1021/nl0733785

[PubMed Abstract](https://pubmed.ncbi.nlm.nih.gov/18386912) | [CrossRef Full Text](https://doi.org/10.1021/nl0733785) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=Y.+Liu&author=W.+Qian&author=Q.+Zhang&author=A.+Cao&author=Z.+Li&author=W.+Zhou+&publication_year=2008&title=Hierarchical+agglomerates+of+carbon+nanotubes+as+high-pressure+cushions&journal=J.+Nano+Lett.&volume=8&pages=1323-1327)

Liu, Y., Xu, Z., Gao, W., Cheng, Z., and Gao, C. (2017). Graphene and other 2D colloids: liquid crystals and macroscopic fibers. *J. Adv. Mater.* 29: 1606794. doi: 10. 1002/adma. 201606794

[PubMed Abstract](https://pubmed.ncbi.nlm.nih.gov/28233348) | [CrossRef Full Text](https://doi.org/10.1002/adma.201606794) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=Y.+Liu&author=Z.+Xu&author=W.+Gao&author=Z.+Cheng&author=C.+Gao+&publication_year=2017&title=Graphene+and+other+2D+colloids%3A+liquid+crystals+and+macroscopic+fibers&journal=J.+Adv.+Mater.&volume=29&pages=1606794)

Ma, R. Z., Wu, J., Wei, B. Q., Liang, J., and Wu, D. H. (1998). Processing and properties of carbon nano-tubes-nano-SiC ceramic. *J. Mater Sci.* 33, 5243–5246. doi: 10. 1023/A: 1004492106337

[CrossRef Full Text](https://doi.org/10.1023/A: 1004492106337) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=R.+Z.+Ma&author=J.+Wu&author=B.+Q.+Wei&author=J.+Liang&author=D.+H.+Wu+&publication_year=1998&title=Processing+and+properties+of+carbon+nano-tubes-nano-SiC+ceramic&journal=J.+Mater+Sci.&volume=33&pages=5243-5246)

Mehdi, M. R., Kim, M., Seong, J. C., and Arsalan, M. H. (2011). Spatio-temporal patterns of road traffic noise pollution in Karachi, Pakistan. *Environ. Int* . 37, 97–104. doi: 10. 1016/j. envint. 2010. 08. 003

[PubMed Abstract](https://pubmed.ncbi.nlm.nih.gov/20851468) | [CrossRef Full Text](https://doi.org/10.1016/j.envint.2010.08.003) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=M.+R.+Mehdi&author=M.+Kim&author=J.+C.+Seong&author=M.+H.+Arsalan+&publication_year=2011&title=Spatio-temporal+patterns+of+road+traffic+noise+pollution+in+Karachi,+Pakistan&journal=Environ.+Int&volume=37&pages=97-104)

Mittal, V., and Chaudhry, A. U. (2015). Polymer - graphene nanocomposites: effect of polymer matrix and filler amount on properties. *J. Macromol. Mat. Eng* . 300, 510–521. doi: 10. 1002/mame. 201400392

[CrossRef Full Text](https://doi.org/10.1002/mame.201400392) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=V.+Mittal&author=A.+U.+Chaudhry+&publication_year=2015&title=Polymer+-+graphene+nanocomposites%3A+effect+of+polymer+matrix+and+filler+amount+on+properties&journal=J.+Macromol.+Mat.+Eng&volume=300&pages=510-521)

Nieto, A., Bisht, A., Lahiri, D., Zhang, C., Agarwal, A. (2016). Graphene reinforced metal and ceramic matrix composites. *J. Intern. Mater. Rev* . 62, 241–302. doi: 10. 1080/09506608. 2016. 1219481

[CrossRef Full Text](https://doi.org/10.1080/09506608.2016.1219481) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=A.+Nieto&author=A.+Bisht&author=D.+Lahiri&author=C.+Zhang&author=A.+Agarwal+&publication_year=2016&title=Graphene+reinforced+metal+and+ceramic+matrix+composites&journal=J.+Intern.+Mater.+Rev&volume=62&pages=241-302)

Nine, M. J., Ayub, M., Zander, A. C., Tran, D. N. H., Cazzolato, B. S., Losic, D. (2017). Graphene oxide-based lamella network for enhanced sound absorption. *J. Adv. Funct. Mater.* 27, 1703820. 1–1703820. 10. doi: 10. 1002/adfm. 201703820

[CrossRef Full Text](https://doi.org/10.1002/adfm.201703820) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=M.+J.+Nine&author=M.+Ayub&author=A.+C.+Zander&author=D.+N.+H.+Tran&author=B.+S.+Cazzolato&author=D.+Losic+&publication_year=2017&title=Graphene+oxide-based+lamella+network+for+enhanced+sound+absorption&journal=J.+Adv.+Funct.+Mater.&volume=27&pages=1703820.1-1703820.10)

Park, S. J., and Kim, B. J. (2010). “ Carbon fibers and their composites,” in *Carbon Fibers Springer Series in Materials Science, Vol 210* (Dordrecht: Springer press), 275–317.

[Google Scholar](http://scholar.google.com/scholar_lookup?author=S.+J.+Park&author=B.+J.+Kim+&publication_year=2010&title=“ Carbon+fibers+and+their+composites,”&journal=Carbon+Fibers+Springer+Series+in+Materials+Science,+Vol+210&pages=275-317)

Qamoshi, K., and Rasuli, R. (2016). Subwavelength structure for sound absorption from graphene oxide-doped polyvinylpyrrolidone nanofibers. *Appl. Phys* . 122: 788. doi: 10. 1007/s00339-016-0332-0

[CrossRef Full Text](https://doi.org/10.1007/s00339-016-0332-0) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=K.+Qamoshi&author=R.+Rasuli+&publication_year=2016&title=Subwavelength+structure+for+sound+absorption+from+graphene+oxide-doped+polyvinylpyrrolidone+nanofibers&journal=Appl.+Phys&volume=122&pages=788)

Rodrfguez-Mirasol, J., Thrower, P. A., and Radovic, L. R. (1993). On the oxidation resistance of C/C composites obtained by liquid-phase impregnation/carbonization of different carbon clothes. *Carbon* 31789: 799. doi: 10. 1016/0008-6223(93)90017-5

[CrossRef Full Text](https://doi.org/10.1016/0008-6223(93)90017-5) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=J.+Rodrfguez-Mirasol&author=P.+A.+Thrower&author=L.+R.+Radovic+&publication_year=1993&title=On+the+oxidation+resistance+of+C%2FC+composites+obtained+by+liquid-phase+impregnation%2Fcarbonization+of+different+carbon+clothes&journal=Carbon&volume=31789&pages=799)

Ruland, W. (1990). Carbon Fibers. *Adv. Mater.* . 2, 528–536. doi: 10. 1002/adma. 19900021104

[CrossRef Full Text](https://doi.org/10.1002/adma.19900021104) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=W.+Ruland+&publication_year=1990&title=Carbon+Fibers&journal=Adv.+Mater.&volume=2&pages=528-536)

Sarkar, S., Sen, S., Mishra, S. C., Kudelwar, M. K., and Mohan, S. (2009). Studies on aluminum – fly-ash composite produced by impeller mixing. *J. Reinforced Plastics Comp.* 29, 144–148. doi: 10. 1177/0731684408096428

[CrossRef Full Text](https://doi.org/10.1177/0731684408096428) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=S.+Sarkar&author=S.+Sen&author=S.+C.+Mishra&author=M.+K.+Kudelwar&author=S.+Mohan+&publication_year=2009&title=Studies+on+aluminum+–+fly-ash+composite+produced+by+impeller+mixing&journal=J.+Reinforced+Plastics+Comp.&volume=29&pages=144-148)

Sheehan, J. E., Buesking, K. W., and Sullivan, B. J. (1994). Carbon-carbon composites. *Annu. Rev. Mater. sci.* 24, 19–44. doi: 10. 1146/annurev. ms. 24. 080194. 000315

[CrossRef Full Text](https://doi.org/10.1146/annurev.ms.24.080194.000315) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=J.+E.+Sheehan&author=K.+W.+Buesking&author=B.+J.+Sullivan+&publication_year=1994&title=Carbon-carbon+composites&journal=Annu.+Rev.+Mater.+sci.&volume=24&pages=19-44)

Shen, Y., and Jiang, G. M. (2014a). Effects of different parameters on acoustic properties of activated carbon fiber felts. *J. Textile Institute* 105, 392–397. doi: 10. 1080/00405000. 2013. 813665

[CrossRef Full Text](https://doi.org/10.1080/00405000.2013.813665) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=Y.+Shen&author=G.+M.+Jiang+&publication_year=2014a&title=Effects+of+different+parameters+on+acoustic+properties+of+activated+carbon+fiber+felts&journal=J.+Textile+Institute&volume=105&pages=392-397)

Shen, Y., and Jiang, G. M. (2014b). Sound absorption properties of composite structure with activated carbon fiber felts. *J. Textile Institute* 105, 1100–1107. doi: 10. 1080/00405000. 2014. 899080

[CrossRef Full Text](https://doi.org/10.1080/00405000.2014.899080) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=Y.+Shen&author=G.+M.+Jiang+&publication_year=2014b&title=Sound+absorption+properties+of+composite+structure+with+activated+carbon+fiber+felts&journal=J.+Textile+Institute&volume=105&pages=1100-1107)

Shen, Y., and Jiang, G. M. (2016). The influence of production parameters on sound absorption of activated carbon fiber felts. *J. Textile Institute* 107, 1144–1149. doi: 10. 1080/00405000. 2015. 1097083

[CrossRef Full Text](https://doi.org/10.1080/00405000.2015.1097083) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=Y.+Shen&author=G.+M.+Jiang+&publication_year=2016&title=The+influence+of+production+parameters+on+sound+absorption+of+activated+carbon+fiber+felts&journal=J.+Textile+Institute&volume=107&pages=1144-1149)

Shukla, S., Roy, A. K., and Kumar, K. (2015). Material selection for blades of mixed flow pump impeller using ANSYS. *Mater. Today* 2, 4–5. doi: 10. 1016/j. matpr. 2015. 07. 172

[CrossRef Full Text](https://doi.org/10.1016/j.matpr.2015.07.172) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=S.+Shukla&author=A.+K.+Roy&author=K.+Kumar+&publication_year=2015&title=Material+selection+for+blades+of+mixed+flow+pump+impeller+using+ANSYS&journal=Mater.+Today&volume=2&pages=4-5)

Singh, V., Joung, D., Zhai, L., Das, S., Khondaker, S. I., and Seal, S. (2011). Graphene based materials: past, present and future. *Prog. Mater. Sci* . 56, 1178–1271. doi: 10. 1016/j. pmatsci. 2011. 03. 003

[CrossRef Full Text](https://doi.org/10.1016/j.pmatsci.2011.03.003) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=V.+Singh&author=D.+Joung&author=L.+Zhai&author=S.+Das&author=S.+I.+Khondaker&author=S.+Seal+&publication_year=2011&title=Graphene+based+materials%3A+past,+present+and+future&journal=Prog.+Mater.+Sci&volume=56&pages=1178-1271)

Stankovich, S., Dikin, D. A., Dommett, G. H. B., Kohlhaas, K. M., Zimney, E. J., Stach, E. A., et al. (2006). Graphene-based composite materials. *J. Nature.* 442, 282–286. doi: 10. 1038/nature04969

[PubMed Abstract](https://pubmed.ncbi.nlm.nih.gov/16855586) | [CrossRef Full Text](https://doi.org/10.1038/nature04969) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=S.+Stankovich&author=D.+A.+Dikin&author=G.+H.+B.+Dommett&author=K.+M.+Kohlhaas&author=E.+J.+Zimney&author=E.+A.+Stach+&publication_year=2006&title=Graphene-based+composite+materials&journal=J.+Nature.&volume=442&pages=282-286)

Stephen, A. S., and Mark, P. M. (2003). Noise pollution: non-auditory effects on health. *Br. Med. Bull* . 68, 243–257. doi: 10. 1093/bmb/ldg033

[PubMed Abstract](https://pubmed.ncbi.nlm.nih.gov/14757721) | [CrossRef Full Text](https://doi.org/10.1093/bmb/ldg033) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=A.+S.+Stephen&author=P.+M.+Mark+&publication_year=2003&title=Noise+pollution%3A+non-auditory+effects+on+health&journal=Br.+Med.+Bull&volume=68&pages=243-257)

Sudeshna, P., Veettil, V. T., and Narayanan, T. N. (2017). Enhanced viscoelastic properties of graphene oxide membranes. *Carbon N. Y* . 124, 576–583. doi: 10. 1016/j. carbon. 2017. 09. 017

[CrossRef Full Text](https://doi.org/10.1016/j.carbon.2017.09.017) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=P.+Sudeshna&author=V.+T.+Veettil&author=T.+N.+Narayanan+&publication_year=2017&title=Enhanced+viscoelastic+properties+of+graphene+oxide+membranes&journal=Carbon+N.+Y&volume=124&pages=576-583)

Suhr, J., and Koratkar, N. (2008). Energy dissipation in carbon nanotube composites. *Mater. Sci.* 43, 4370–4382. doi: 10. 1007/s10853-007-2440-x

[CrossRef Full Text](https://doi.org/10.1007/s10853-007-2440-x) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=J.+Suhr&author=N.+Koratkar+&publication_year=2008&title=Energy+dissipation+in+carbon+nanotube+composites&journal=Mater.+Sci.&volume=43&pages=4370-4382)

Sun, X., Jia, X., Liu, J., Wang, G., Zhao, S., Ji, L., et al. (2020a). Investigation on the characteristics of an advanced rotational hydrodynamic cavitation reactor for water treatment. *Sep. Purif. Technol.* 2020: 117252. doi: 10. 1016/j. seppur. 2020. 117252

[CrossRef Full Text](https://doi.org/10.1016/j.seppur.2020.117252) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=X.+Sun&author=X.+Jia&author=J.+Liu&author=G.+Wang&author=S.+Zhao&author=L.+Ji+&publication_year=2020a&title=Investigation+on+the+characteristics+of+an+advanced+rotational+hydrodynamic+cavitation+reactor+for+water+treatment&journal=Sep.+Purif.+Technol.&volume=2020&pages=117252)

Sun, X., Liu, J., Ji, L., Wang, G., Zhao, S., Yoon, J. Y., et al. (2020b). A review on hydrodynamic cavitation disinfection: the current state of knowledge. *Sci. Total Environ.* 2020: 139606. doi: 10. 1016/j. scitotenv. 2020. 139606

[PubMed Abstract](https://pubmed.ncbi.nlm.nih.gov/32783818) | [CrossRef Full Text](https://doi.org/10.1016/j.scitotenv.2020.139606) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=X.+Sun&author=J.+Liu&author=L.+Ji&author=G.+Wang&author=S.+Zhao&author=J.+Y.+Yoon+&publication_year=2020b&title=A+review+on+hydrodynamic+cavitation+disinfection%3A+the+current+state+of+knowledge&journal=Sci.+Total+Environ.&volume=2020&pages=139606)

Tang, J., Zhou, H., Liang, Y., Shi, X., Yang, X., and Zhang, J. (2014). Properties of graphene oxide/epoxy resin composites[J]. *Journal of Nanomaterials.* 2014, 1–5. doi: 10. 1155/2014/696859

[CrossRef Full Text](https://doi.org/10.1155/2014/696859)

Verdejo, R., Pfli, R., Alvarez-Lainez, M., Mourad, S., Rodriguez-Perez, M. A., et al. (2009). Enhanced acoustic damping in flexible polyurethane foams filled with carbon nanotubes. *Compos. Sci. Technol* . 69, 1564–1569. doi: 10. 1016/j. compscitech. 2008. 07. 003

[CrossRef Full Text](https://doi.org/10.1016/j.compscitech.2008.07.003) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=R.+Verdejo&author=R.+Pfli&author=M.+Alvarez-Lainez&author=S.+Mourad&author=M.+A.+Rodriguez-Perez+&publication_year=2009&title=Enhanced+acoustic+damping+in+flexible+polyurethane+foams+filled+with+carbon+nanotubes&journal=Compos.+Sci.+Technol&volume=69&pages=1564-1569)

Willemsen, A. M., and Rao, M. D. (2015). Sound absorption characteristics of nanocomposite polyurethane foams infused with carbon nanotubes. *Noise Control Eng.* 63, 424–438. doi: 10. 3397/1/376338

[CrossRef Full Text](https://doi.org/10.3397/1/376338) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=A.+M.+Willemsen&author=M.+D.+Rao+&publication_year=2015&title=Sound+absorption+characteristics+of+nanocomposite+polyurethane+foams+infused+with+carbon+nanotubes&journal=Noise+Control+Eng.&volume=63&pages=424-438)

Wu, G., Liu, Y., Xiu, Z., Jiang, L., and Yang, W. (2010). Reaction procedure of a graphite fiber reinforced Ti-Al composite produced by squeeze casting-in situ reaction. *J. Rare Metals.* 1, 100–103. doi: 10. 1007/s12598-010-0017-3

[CrossRef Full Text](https://doi.org/10.1007/s12598-010-0017-3) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=G.+Wu&author=Y.+Liu&author=Z.+Xiu&author=L.+Jiang&author=W.+Yang+&publication_year=2010&title=Reaction+procedure+of+a+graphite+fiber+reinforced+Ti-Al+composite+produced+by+squeeze+casting-in+situ+reaction&journal=J.+Rare+Metals.&volume=1&pages=100-103)

Xie, S. C., Yang, S. C., Yang, C. X., and Wang, D. (2020). Sound absorption performance of a filled honeycomb composite structure. *Appl. Acoust* . 162: 214. doi: 10. 1016/j. apacoust. 2019. 107202

[CrossRef Full Text](https://doi.org/10.1016/j.apacoust.2019.107202) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=S.+C.+Xie&author=S.+C.+Yang&author=C.+X.+Yang&author=D.+Wang+&publication_year=2020&title=Sound+absorption+performance+of+a+filled+honeycomb+composite+structure&journal=Appl.+Acoust&volume=162&pages=214)

Yang, M., and Sheng, P. (2017). Sound absorption structures: from porous media to acoustic metamaterials. *Annu. Rev. Mater. Res* . 47, 83–114. doi: 10. 1146/annurev-matsci-070616-124032

[CrossRef Full Text](https://doi.org/10.1146/annurev-matsci-070616-124032) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=M.+Yang&author=P.+Sheng+&publication_year=2017&title=Sound+absorption+structures%3A+from+porous+media+to+acoustic+metamaterials&journal=Annu.+Rev.+Mater.+Res&volume=47&pages=83-114)

Yang, X. C., Bai, P. F., Shen, X. M., To, S., Chen, L., Zhang, X. N., et al. (2019). Optimal design and experimental validation of sound absorbing multilayer microperforated panel with constraint conditions. *Appl. Acoust* . 146, 334–344. doi: 10. 1016/j. apacoust. 2018. 11. 032

[CrossRef Full Text](https://doi.org/10.1016/j.apacoust.2018.11.032) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=X.+C.+Yang&author=P.+F.+Bai&author=X.+M.+Shen&author=S.+To&author=L.+Chen&author=X.+N.+Zhang+&publication_year=2019&title=Optimal+design+and+experimental+validation+of+sound+absorbing+multilayer+microperforated+panel+with+constraint+conditions&journal=Appl.+Acoust&volume=146&pages=334-344)

Young, R. J., Kinloch, I. A., Gong, L., and Novoselov, K. S. (2012). The mechanics of graphene nanocomposite: a review. *J. Compos. Sci. Technol.* 72, 1459–1476. doi: 10. 1016/j. compscitech. 2012. 05. 005

[CrossRef Full Text](https://doi.org/10.1016/j.compscitech.2012.05.005) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=R.+J.+Young&author=I.+A.+Kinloch&author=L.+Gong&author=K.+S.+Novoselov+&publication_year=2012&title=The+mechanics+of+graphene+nanocomposite%3A+a+review&journal=J.+Compos.+Sci.+Technol.&volume=72&pages=1459-1476)

Zhang, Q., Zhao, M., Liu, Y., Cao, A., Qian, W., Lu, Y., et al. (2009). Energy-absorbing hybrid composites based on alternate carbon-nanotubes and inorganic layers. *J. Adv. Mater* . 21, 2876–2880. doi: 10. 1002/adma. 200900123

[CrossRef Full Text](https://doi.org/10.1002/adma.200900123) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=Q.+Zhang&author=M.+Zhao&author=Y.+Liu&author=A.+Cao&author=W.+Qian&author=Y.+Lu+&publication_year=2009&title=Energy-absorbing+hybrid+composites+based+on+alternate+carbon-nanotubes+and+inorganic+layers&journal=J.+Adv.+Mater&volume=21&pages=2876-2880)

Zhang, R., Wen, Q., Qian, W., Su, D. S., Zhang, Q., and Wei, F. (2011). Superstrong ultralong carbon nanotubes for mechanical energy storage. *J. Adv. Mater.* 23, 3387–3391. doi: 10. 1002/adma. 201100344

[PubMed Abstract](https://pubmed.ncbi.nlm.nih.gov/21671453) | [CrossRef Full Text](https://doi.org/10.1002/adma.201100344) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=R.+Zhang&author=Q.+Wen&author=W.+Qian&author=D.+S.+Su&author=Q.+Zhang&author=F.+Wei+&publication_year=2011&title=Superstrong+ultralong+carbon+nanotubes+for+mechanical+energy+storage&journal=J.+Adv.+Mater.&volume=23&pages=3387-3391)

Zhang, S. H., and Xu, W. (2011). Absorption of surface acoustic waves by graphene. *AIP Adv* . 1: 022146. doi: 10. 1063/1. 3608045

[CrossRef Full Text](https://doi.org/10.1063/1.3608045) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=S.+H.+Zhang&author=W.+Xu+&publication_year=2011&title=Absorption+of+surface+acoustic+waves+by+graphene&journal=AIP+Adv&volume=1&pages=022146)

Zhao, X. D., Wang, X., and Yu, Y. J. (2018). Enhancing low-frequency sound absorption of microperforated panel absorbers by combining parallel mechanical impedance. *Appl. Acoust* . 130, 300–304. doi: 10. 1016/j. apacoust. 2017. 10. 001

[CrossRef Full Text](https://doi.org/10.1016/j.apacoust.2017.10.001) | [Google Scholar](http://scholar.google.com/scholar_lookup?author=X.+D.+Zhao&author=X.+Wang&author=Y.+J.+Yu+&publication_year=2018&title=Enhancing+low-frequency+sound+absorption+of+microperforated+panel+absorbers+by+combining+parallel+mechanical+impedance&journal=Appl.+Acoust&volume=130&pages=300-304)

Zhou, X., Shin, E., Wang, K. W., and Bakis, C. E. (2004). *Compos. Sci. Technol* . 64: 2425. doi: 10. 1016/j. compscitech. 2004. 06. 001

[CrossRef Full Text](https://doi.org/10.1016/j.compscitech.2004.06.001)